## Slide 1: Two detector XRD pattern acquisition
Monty Cosby

## Slide 2: Experimental setup
Setup
2D area detector fixed at 15˚ 2θ below sample
Single crystal detector attached to goniometer
Acquisition:
Low-res pattern acquired by 2D area detector
Peaks identified in crude pattern
Move crystal detector to peak locations for data collection
Eliminates useless background acquisition
2D area detector
Detector crystal
Incident beam
Diffracted
beam

## Slide 3
Peaks picked from integrated 2D pattern
SciPy peak pickers were poor
Difficult due to background (false peaks and not uniform)
Second derivative not always consistently negative
Peak picking from pattern
non-uniform
“false peaks”
Background issues
Derivative not always negative
Imperfect peaks
PbI2 + ZnO

## Slide 4
Peaks picked from integrated 2D pattern
SciPy peak pickers were poor
Difficult due to background (false peaks and not uniform)
Second derivative not always consistently negative
Current fix:
Smooth out pattern
Future fix:
Remove background with blank
Smooth out pattern
Peak picking from pattern
Background issues
Imperfect peaks
less random,
discriminable
smoothed
original

## Slide 5
Code runs in ~1 s
  Will improve after removing unnecessary visualization
  Worsen with added integration
Hit/miss at high 2θ
Only a few mis picked peaks, one peak not picked by code
Will be easier to discriminate for smaller data region
Peaks picked by python script
Circled are false positives for less than 40˚
PbI2 + ZnO
February 2022

## Slide 6
Will need to convert 2θ from 2D area detector to crystal
Preliminary experiment should be run to determine the appropriate 2D area detector distance
  Can use current setup by moving the detector to 15˚ and sliding closer to the sample to compare the patterns
  Will give a good indication of ability to peak pick/smooth and if background subtraction is possible
The detector distance problem
2D area detector
Detector crystal
Peaks vs noise

## Slide 7
Will need to convert 2θ from 2D area detector to crystal
Preliminary experiment should be run to determine the appropriate 2D area detector distance
  Can use current setup by moving the detector to 15˚ and sliding closer to the sample to compare the patterns
  Will give a good indication of ability to peak pick/smooth and if background subtraction is possible
The detector to distance problem
2D area detector
Detector crystal
Peaks vs noise
If efficient (and can move the detector distance from the bottom) ex situ measurements can be easily taken during the time
Low temperature melting or crystallization can be followed easily